## Slide 2
Virtual atoms in semiconductors
Understanding behaviours of defects in wide bandgap semiconductors for using as virtual atoms.
Deterministic implantation and defect electro-optical handling

## Slide 3
NV-spin state can be initialized optically by laser
NV-spin state can be coherently manipulated with resonant microwave (MW) fields
NV-spin state can be read out optically by its spin-state-dependent fluorescence, enabling optically detected magnetic resonance experiments.
The system enables the realization of a fully functional qubit which interacts with its environment and results in an optically readable signal.

## Slide 4
FIB COLUMN
LIQUID METAL ALLOY ION SOURCE
Si++; Au++; Au+
Ge+ or Ge++
ION ENERGY (ACC. VOLTAGE: 2 -35 kV):
2 -35 keV for SINGLE CHARGED ions;
4 –70 keV for DOUBLE CHARGED ions.
LMAIS ION BEAM INTENSITY:
Si++: min. 1.5 pA; max. 475 pA
Ge+: min. 1.3 pA; max. …
Ge: min. 1.9 pA; max. 420 pA
Au+: min. 4.1 pA; max. 2,000 pA
Au++: min. 1.7 pA; max. 420 pA
PATTERN GENERATOR: 20 bit/ 50 MHz
MINIMUM DWELL TIME: 20 ns
MINIMUM STEP SIZE: 0.2 nm on 200 µm WF
LASER INTERFEROMETER TABLE
EXCELLENT STITCHING AND BLIND NAVIGATION
SMALL SAMPLES preferred
TILT 0-90°ON 1.5x1.5 cm2
A NANOFABRICATION MACHINE
Deterministic implantation

## Slide 5: Ion Dose makes the difference for applications: sputtering yield and milled depth 70 keV Ge+ on Si - collision cascade (SRIM simulations)
Si SURFACE
ρ = Atomic Density,
Y = Ion Species, Energy and Angle
ION DOSE
MILLED DEPTH
SINGLE ION IMPLANTATION;
single vacancy-complexes.
ION IMPLANTATION:
  composition change
  defect creation
  amorphization
ION MILLING:
  sputtering
  patterning.
1-100 ions per spot
1E13-1E16 ions/ cm2
6E15 - … ions/ cm2
INCREASING ION DOSE
ION INDUCED (NANO-) STRUCTURES:
  ripples, hillocks, terraces…
  nanovoid
  self-assembly

## Slide 6
Confocal fluorescence scans of a SiC surface impl. with Si++
100 ions/spot
400 ions/spot
Deterministic implantation: scattering implantation

## Slide 7
Lithography defined implantation
Particle beam

## Slide 8
We successfully built a confocal microscopy system for the detection of the PL from both NV- and SiV
Optical cryo-setup